**SECTION 12 48 16**

**Entrance Grille - Profile Bar with Genuine SLIPNOT**

**Guidance - Specifier please choose (1) option in each of the highlighted areas and remove remaining choices.**

**PART 1: General**

**1.1 Summary**

Provide stainless steel grating panels as shown and specified, in accordance with the requirements of the Contract Documents and Drawings.

**1.2 Related Sections**

 Section XXXX – Submittals

**1.3 Submittals**

1. Submit a Quality Manual showing evidence of being an ISO 9001 certified company.
2. Submit shop drawings showing compliance with the specifications including layout of unit with required sectioning, framing, support system, mounting type and locations along with tolerances, prior to manufacturing of grating.
3. Submit design calculations, by a registered ENGINEER, including loading conditions, support design, and deflection calculations of the stainless-steel grating panels.
4. 4" x 4" standard sample size can be submitted for verification purposes.

**1.4 Warranty**

1. Manufacturing Warranty Period: One year from acceptance and furnishing owner items found to be defective within the one-year period.
2. Extended warranties are available at additional cost and must be approved by management prior to receipt of purchase order.

**1.5 Quality Assurance**

1. Grating shall be manufactured by an ISO 9001-2015 Certified company, fabricated by ASME Section IX Certified welders.

**PART 2: Products**

**2.01 Manufacturers**

1. **Hendrick Architectural Products**, Carbondale, PA email: sales@hendrickarchproducts.com, phone: 877-840-0881, fax: 570-282-1506

**2.02 Materials**

1. Construction: Floor Panels shall consist of precision spaced, mechanically interlocked profile wires and U-clip support from Type 304 or 316 stainless steel. The traffic surface shall be of smooth profile bar shape with inwardly enlarging openings to minimize the likelihood of debris entrapment.
2. Genuine SLIPNOT coating on 1/2" or 1-1/4" wide bars evenly spaced throughout unit with max. 4" spacing or on Alternating profile bar or on full top surface of unit.
3. The bars, U-clips, mounting brackets and banding shall be welded to form a single unit as shown on the drawings.
4. Bars to be B-9S, B-9, B-12S, B-12, B-16, T-9M or T-16 and mechanically interlocked using a U-clip support structure and spaced .187 (4.75mm) apart.
5. The area for this opening shall be 57.19%. Opening size shall be controlled and continuously monitored during manufacture.
6. The maximum opening between the wires is 3/16” to be high heel safe.
7. The direction of walking or flow must be perpendicular to the wire direction.
8. Supports: U-clip supports will be spaced on approx. 3" centers.

**2.03 Mounting**

1. (a) Hidden Mounting Tabs with slotted holes type 304 or 316 stainless steel to secure screen to concrete surface. (b) Surface mounted hold downs (c) EZ Loc Mounting

**2.04 Performance**

1. Entrance grilles capable of withstanding 300 lb./sf pedestrian load, 1000 lb. rolling load using a 5" diameter x 2" wide polyurethane tread for 1,000 passes.
2. Entrance grilles with Genuine SLIPNOT provide maximum traction with maximum durability providing long-term safety with a single installation. SLIPNOT surfaces provide wet dynamic coefficient of friction (DCOF) values exceeding 0.90, over double the ANSI/NFSI minimum recommended value of 0.42 and a minimum and Static Coefficient of Friction (SCOF) of 1.1 using Neo lite in wet and dry applications where minimum recommended value of 0.60.
3. Tolerances: Panels shall be designed and fabricated so as to ensure that the completed tread panels are within the tolerances specified herein while under a no-load condition: Panel length and width shall be within 1/8 inch plus or minus.

**Part 3: Execution**

**3.01 Examination**

1. A. Verification of conditions: Examine areas and conditions under which work is to be performed and identify conditions detrimental to proper or timely completion.

 1. Do not proceed until unsatisfactory conditions have been corrected.

**3.02 Preparation**

1. Manufacturer shall offer assistance and guidance to provide a template of irregular shaped grid assemblies to ensure a proper installation.

**3.03 Installation**

1. Install the work of this section in strict accordance with the manufacturer’s recommendations.
2. Set grid type at height recommended by manufacturer for most effective cleaning action.
3. Coordinate the top of grid surfaces with bottom of doors that swing across to provide ample clearance between door and grid.

**3.04 Cleaning**

1. A. Clean the tread surface and recessed well as frequently as recommended by manufacturer to reduce the effects of accumulated soiling that may hinder performance and lifetime.

**3.05 Protection**

1. After Installation of frame and concrete work It Is recommended to provide a temporary filler until surrounding work Is complete.
2. Final Installation of floor grating should not take place until project has reached substantial completion stage.

**END OF SECTION**